## Slide 1
MOF Membranes： Synthesis，Adsorption for Green Application
Shilun Qiu
The State Key Laboratory of Inorganic Synthesis and Preparetive Chemistry, Jilin University, Changchun,CHINA
Email-sqiu@jlu.edu.cn
April 28, IYCr, Karachi

## Slide 3
Chemistry Building
Jilin University
Main Campus
Typical Scene
in Changchun
SKL Inorg. Synth. & Prep. Chem.

## Slide 4: Outline
Conclusion
Applications for green chemistry
1. Sensors
2. Separations
3. Devices
4. Chiral resolution
Synthesis approaches for MOF membranes
1. In-situ
2. Seeded growth
3. Microwave
4. Interfacial synthesis
5. Contra-diffusion synthesis
Brief introduction of Porous materials and Membrane

## Slide 5
Ordered porous materials
COFs (Covalent Organic Framework )
Zeolite & Mesoporous Silica（Inorganic）
MOFs （ Coordination Polymers）

## Slide 6
Porous Materials
Molecular
Separation
Hydrogen Storage
Molecular Magnet
Optical Materials
Gas Separation
Catalytic Materials
Applications

## Slide 7
A variety of Membranes and Films
of various thickness, with homogeneous or heterogeneous structure.
classified according to pore diameter.
Membranes can be
Cell membrane
Hollow fiber
liquid membrane
Egg shell membrane
Solar energy film
Filter membrane
Film to the glass
Reverse osmosis membrane

## Slide 8
Superiority of Membranes and Films compared to powder materials
Recyclable
High
efficiency
Continuous
work
Energy
saving
Easy to
operate

## Slide 9
Microwave
Contra-diffusion synthesis
Interfacial synthesis
Vapor phase
Seeded growth
In-situ
Layer-by-layer preparation
Thermally induced
phase separation
Molten state stretching
under stress
Immersion precipitation
phase transformation
Porous Membranes and films
Membranes and films
Synthesis approaches of membranes and films
Zeolites
MOFs
Membranes and films
Polymer
Membranes and films

## Slide 10
Self-Assembled Organic Monolayers (SAMs)
In-situ method
R.A. Fischer, etc. J. Am. Chem. Soc., 2005, 127, 13744-13745
Anchoring a typical MOF-5 building unit to a carboxylic acid-terminated SAM.
Optical microscope (left) and an AFM image (right) of a selectively grown MOF-5 film on a patterned SAM of 16-mercaptohexadecanoic acid and 1H,1H,2H,2H-perfluorododecane thiol on Au(111).
MOF-5 film

## Slide 11
H. Bux, F. Liang, Y. Li, J. Cravillon, M. Wiebcke and J. Caro, Journal of the American Chemical Society, 2009, 131, 16000.
(left) SEM image of the cross section of a simply broken ZIF-8 membrane.
(right) EDXS mapping of the sawn and polished ZIF-8 membrane (color code: orange, Zn; cyan, Ti).
ZIF-8 membrane
Microwave synthesis

## Slide 12
Layer-by-layer (LbL) growth of MOF A and MOF B
O. Shekhah, H. Wang, D. Zacher, R. A. Fischer, Angew. Chem. Int. Ed. 2009, 48, 5038.
S. Furukawa, K. Hirai, Y. Takashima, K. Nakagawa, M. Kondo, T. Tsuruoka, O. Sakata, S. Kitagawa, Chem. Commun. 2009, 5097.
Layer-by-layer preparation
Layer-by-layer (LbL) growth of MOFs on SAMs by repeated growth cycles: immersion in a solution of metal precursor, washing, immersion in a solution of the organic ligand, washing.

## Slide 13
Interfacial synthesis
Interfacial preparation of a MOF layer using a biphasic synthesis mixture: an aqueous metal-ion-containing solution (blue) and an organic ligand solution (purple).
A thin film of ZIF-8 obtained by layering a solution of the ligand in 1-octanol on top of an aqueous zinc nitrate solution.
A thin film of [Cu3(BTC)2] was obtained by layering a solution of the ligand in 1-octanol on top of an aqueous cupric acetate solution
Dirk E. De Vos, etc., Nature Chemistry, 2011, 3, 382-387
Deposition of MOF layer on a support (brown) in a homogeneous mixture. Undesired nucleation can occur.
HKUST-1 and ZIF-8 membrane

## Slide 14
ZIF-8 membrane
Contra-diffusion synthesis
SEM images of ZIF-8 films prepared on nylon membranes for 16 h (a, d), 24 h (b, e), and 72 h (c, f). Zinc solution side (a–c) and Hmim solution side (d–f).
(a) Diffusion cell for ZIF-8 film preparation; (b) schematic formation of ZIF-8 films on both sides of the nylon support. (Hmim = 2-methylimidazolate)
Cross-section SEM image of the ZIF-8 film at the zinc nitrate solution side.
H. Wang, Chem. Commun., 2011, 47, 2559–2561

## Slide 15
Separation
Devices
Chiral Resolution
Low-κ dielectrics
Sensor
Porous Membranes and Films in our group

## Slide 16
Twin Copper Source
Optic micrographs of (a) copper net and (b) net-supported Cu3(BTC)2 membrane; SEM image of (c) the surface and (d) cross section of the membrane.
Hailing Guo, Guangshan Zhu, Ian J. Hewitt, and Shilun Qiu, J. AM. CHEM. SOC. 2009, 131, 1646–1647
Plot of H2/N2,H2/CH4 and H2/CO2 separation factor of the copper net supported Cu3(BTC)2 membrane with change in test time.
HKUST-1 membrane
In-situ (direct synthesis) method
Separation

## Slide 17
ZIF-8 membrane
Schematic diagram of the electrospinning process for (a) planar support (macroporous SiO2 wafer) and (b) tube support (porous Al2O3 tube) seeding.
(a)
(b)
Lili Fan, Ming Xue, Zixi Kang, Huan Li, Shilun Qiu J. Mater. Chem., 2012, 22, 25272–25276
Introduced into the synthesis of supported microporous membranes for the first time
1. Suitable for various substrates, especially tubes
2. With possibility of large-area processing
3. Precisely control the thickness of the seed layer
4. Uniform seed coating on the support surface
Advantages :
Electrospinning
Separation

## Slide 18
ZIF-8 has a sodalite (SOD) zeolite-type structure with 3.4 Å small aperture. The remarkable thermal and chemical stability, as well as the simple synthetic steps make it an ideal candidate.
SEM images of the PVP fibers from concentrations of methanol solutions: (a) 8%, (b) 9%, (c) 10%, (d) 11%, (e) 12%, and (f) 13%.
✓
SEM images of ZIF-8/PVP composite fibers electrospun from methanol solutions of 12 wt% PVP and different seed concentrations (a) 6 wt%, (b) 8 wt%, (c) 10 wt% and (d) 12 wt%.
✓
85nm
ZIF-8 membrane
Electrospinning
Lili Fan, Ming Xue, Zixi Kang, Huan Li, Shilun Qiu J. Mater. Chem., 2012, 22, 25272–25276
Separation

## Slide 19
simulated ZIF-8
ZIF-8 seeds
ZIF-8 membrane
XRD patterns of the simulated ZIF-8 (a), ZIF-8 seeds (b) and synthesized ZIF-8 membrane (c).
ZIF-8 membrane
Electrospinning
Table Permeance (molm-2 s-1Pa-1) and separation factors (H2 versus other gases) of the ZIF-8 membrane at 298 K and 1 atmospheric pressure. The volume ratio for the mixed gas systems is 1 : 1
Plot of H2/CO2, H2/N2 and H2/CH4 separation factors of the ZIF-8 membrane with changes in testing time.
SiO2 wafer
Al2O3 tube
membrane
membrane
SEM images of the support surface (a), top-view of the ZIF-8 membrane without (b) and with (c and d) seeding fibers, cross-section view of the ZIF-8 membrane (e and f).
Lili Fan, Ming Xue, Zixi Kang, Huan Li, Shilun Qiu J. Mater. Chem., 2012, 22, 25272–25276
Separation

## Slide 20
JUC-32 film
Electrospinning
20μm
5μm
1μm
5μm
silica disc
JUC-32 seeds
JUC-32 film
Cross-section
simulated
JUC-32 seeds
JUC-32 film
Separation
Lili Fan, Ming Xue, Zixi Kang, and Shilun Qiu, accepted by Science China Chemistry

## Slide 21
Schematic diagram of preparation of DPPA-loaded SAPO-5 film on quartz support. (DPPA= dimethyl-(4-phenylazophenyl)-amine)
Ming Xue, Lili Fan, Zixi Kang, Wenting Zhang, Huan Li, Shilun Qiu J. Mater. Chem. 2012, 22, 17644–17648
C-oriented SAPO-5 film
Quartz slice
Host-guest system
Sensor

## Slide 22
SEM images of seed crystals (a), c-oriented seed layer (b), c- oriented SAPO-5 film surface (c and d) and cross-section (e and f).
XRD patterns of SAPO-5 seeds (a) and c oriented SAPO-5 film (b).
.
C-oriented SAPO-5 film
Quartz slice
Host-guest system
Ming Xue, Lili Fan, Zixi Kang, Wenting Zhang, Huan Li, Shilun Qiu J. Mater. Chem. 2012, 22, 17644–17648
SAPO-5 seeds
SAPO-5 film
Sensor

## Slide 23
UV absorption spectra of template-free SAPO-5 film (a), dye in ethanol (b) and dye-loaded SAPO-5 film (c).
UV absorption intensity as a function of concentration for Cu2+, Zn2+, Co2+, Pb2+, Cd2+, Hg2+.
C-oriented SAPO-5 film
Host-guest system
Ming Xue, Lili Fan, Zixi Kang, Wenting Zhang, Huan Li, Shilun Qiu J. Mater. Chem. 2012, 22, 17644–17648
SAPO-5 film
Dye
Dye loaded SAPO-5 film
Sensor

## Slide 24
Hydrophobic part
Hydrophilic part
HKUST-1 film
(a) Photo of as-prepared Cu3(BTC)2 film (right: with Al electrodes); SEM images of (b) the surface, (c) surface in magnification, (d) cross-section view
Jia Liu, Fuxing Sun, Feng Zhang, Zhu Wang, Rui Zhang, Ce Wang, Shilun Qiu, J. Mater. Chem. 2011, 21, 3775–3778
Humidity sensing
Pore network of Cu3(BTC)2: (a) View from [100] direction, hydrophilic (dimeric cupric tetracarboxylate units) and hydrophobic (aromatic rings) parts. (b) View from [111] direction.
Capacitance response to the relative humidity (RH) of the film sensor.
Temporal response to different RH of the film sensor.
Copper slice
Sensor

## Slide 25
VOCs sensing
Zn3(BTC)2 film
Xiaoqin Zou, Guangshan Zhu, Ian J. Hewitt, Fuxing Sun, Shilun Qiu, Dalton Trans. 2009, 3009–3013
Zinc slice
Sensor
Schematic representation of typical fabrication of Zn3 (BTC)2 film.
XRD patterns of (a) simulated Zn3(BTC)2 and (b) the film on zinc slice.
SEM images of (a) the film synthesized with H2O2 activation for 6 h; (b) magnified view of (a); (c) and (d) cross-section view at 45◦.

## Slide 26
VOCs sensing
Emission spectra of Zn3(BTC)2 film with different solvents in presence of dimethylamine (λex= 327nm).
Emission spectra of Zn3(BTC)2 film with different concentrations of (a) dimethylamine, methanol and acetone, (b) dimethylamine, n-propylamine, n-butylamine and aniline in ethanol solutions (λex= 327nm).
Emission intensities of Zn3(BTC)2 film after 10 circles with different dimethylamine concentrations in ethanol.
Zn3(BTC)2 film
Sensor
Xiaoqin Zou, Guangshan Zhu, Ian J. Hewitt, Fuxing Sun, Shilun Qiu, Dalton Trans. 2009, 3009–3013

## Slide 27
Eu1−xTbx-MOF films
Luminescent Thin Film
SEM images of Ln-MOFs crystals synthesized: (a) without capping reagent; with addition of (b) sodium oxalate, (c,d) sodium formate and (e,f) sodium acetate.
SEM images of Tb0.5Eu0.5-MOF film viewed from: (a) the surface and (b) the cross section.
XRD patterns of Ln-MOFs. (a) simulated, (b) without capping reagent, (c) with addition of sodium formate, (d) with addition of sodium acetate, and (e) with addition of sodium oxalate.
Hailing Guo, Yongzhong Zhu, Shilun Qiu, Johannes A. Lercher, Hongjie Zhang, Adv. Mater. 2010, 22, 4190–4192
Devices
Spin-coating
simulated
without capping reagent
with sodium formate
with sodium acetate
with sodium oxalate

## Slide 28
Luminescent Thin Film
Photoluminescent spectra of as-prepared Eu1−xTbx-MOF films with Tb3+/Eu3+ mol ratio of: (a) 2.75, (b) 2.44, (c) 1.95 (d) 1.46, (e) 1.02, (f) 0.40 and (g) 0.30.
Comparison of the color of calculated chromaticity with that of the measured (on the right side). Tb3+/Eu3+ mol ratio: (a) 2.75, (b) 2.44, (c) 1.95, (d) 1.46, (e) 1.02, (f) 0.40, (g) 0.30.
Eu1−xTbx-MOF films
Hailing Guo, Yongzhong Zhu, Shilun Qiu, Johannes A. Lercher, Hongjie Zhang, Adv. Mater. 2010, 22, 4190–4192
Tb3+/Eu3+
2.75
2.44
1.95
1.46
1.02
0.40
0.30
2.75
2.44
1.95
1.46
1.02
0.40
0.30
Devices

## Slide 29
Ordered AFI film
Seeded growth
(a) AlPO4-5 structure along the [001] (upper) and [100] (bottom) directions, respectively. (b) Schematic representation of the preparation of the {001} (upper) and {100} (bottom) substrates. (c) Schematic drawing of the epitaxial growth of AlPO4-5 film from the {001} (upper) and {100} (bottom) faces of the substrates.
Rui Xu, Guangshan Zhu, Xiaoju Yin, Xin Wan, Shilun Qiu, J. Mater. Chem. 2006, 16, 2200–2204
Devices

## Slide 30
Seeded growth
Optical micrograph of AlPO4-5 single crystals
XRD patterns of AlPO4-5 film grown on (a) {001} and (b){100} faces of AlPO4-5 crystal substrate.
Different reaction times: (a) after 3 h, (b) 4.5 h, (c) 6 h and (d) the cross-section image of (c) on AlPO4-5 {001} basal face; (e) after 3 h, (f) 4.5 h, (g) 6 h and (h) the cross-section image of (g) on the AlPO4-5 {100} basal face.
Absorption (a) and emission spectra (c) of the AlPO4-5/RhB film and absorption of RhB in aqueous solution (b).
Ordered AFI film
Rui Xu, Guangshan Zhu, Xiaoju Yin, Xin Wan, Shilun Qiu, J. Mater. Chem. 2006, 16, 2200–2204
1mm
3h
4.5h
6h
3h
4.5h
6h
{001}
{100}
Devices

## Slide 31
Ni2(asp)2(bpy) membrane
Schematic diagram of homochiral MOF membranes preparation by in situ growth on nickel nets.
“Single Nickel Source”
(a) Leica picture and (b) SEM pictures of surface of Ni2(L-asp)2(bipy) membrane, (c) detail of the densely packed crystallites, (d) cross-section SEM picture of Ni2(L-asp)2(bipy) membrane
3D frameworof Ni2(L-asp)2(bipy) viewed along the [010] direction. Ni green, C gray (chiral centers yellow), N blue, O red, H white.
Digital photo of the nickel net (left) and the nickel net supported membrane
Chiral
resolution
Memberane based Chiral resolution
L-asp = L-aspartic acid
bipy = 4,4'-Dipyridyl
Zixi Kang, Ming Xue, Lili Fan, Jinying Ding, Lianxun Gao, and Shilun Qiu, in preparation

## Slide 32
P=0.2MPa
P=0.1MPa
Comparison of the ee values for diol mixtures at different temperatures and pressures
Changes of membrane flux with temperature and pressure
Ni2(asp)2(bpy) membrane
Chiral
resolution
Memberane based Chiral resolution
Zixi Kang, Ming Xue, Lili Fan, Jinying Ding, Lianxun Gao, and Shilun Qiu, in preparation

## Slide 33
Scheme 1. (a): Schematic diagram of preparation of the Ni2(L-asp)2P (P = bipy or pz) membranes on nickel nets. (b): Schematic description of compounds 1 and JUC-150 structures. Ni cyan, C gray, N blue, O red; H atoms are omitted for clarity.
Ultra-microporous MOFs Membrane
JUC-150 membrane for gas separation
Kangzi Xi, Ming Xue and Shilun Qiu etc., Energy & Environmental Science (Submitted)

## Slide 34
Kangzi Xi, Ming Xue and Shilun Qiu etc., Energy & Environmental Science (Submitted)

## Slide 36
Financial Support:
National Natural Science Foundation of China (NSFC)
National Basic Research Program of China “973”
Ministry of Science & Technology of China
Ministry of Education of China
Acknowledgment
Prof. Teng Ben, Prof. Guangshan Zhu
Drs. Daliang Zhang, Ming Xue, Hao Ren
PhD students: Cuiying Pei, Lili Fan, Zixi Kang