## Slide 1
a Double Dose: combining Single-Crystal and Powder XRD
for Analysis of Pharmaceutical Materials
Eric Hovestreydt, Arnt Kern, Martin Adam
Bruker AXS GmbH
www.bruker.com

## Slide 2: From Discovery to Production The Applications for X-ray Diffraction
Lead Finding
Optimization
Preclinical
Phase I
Phase II
Phase III
Marketing
XRPD
Discovery
Development
Production
SC-XRD

## Slide 3: X-Ray Techniques
X-ray diffraction techniques
  Single crystal diffraction (SC-XRD)
  Powder diffraction (XRPD)
  Small angle scattering (SAXS)
X-ray imaging
  Computed tomography (CT and micro CT)

## Slide 4: X-Ray Diffraction Techniques Single Crystal Diffraction
Lead Finding
Optimization
Preclinical
Phase I
Phase II
Phase III
Marketing
XRPD
Discovery
Development
Production
SC-XRD

## Slide 5: X-Ray Diffraction Techniques Single Crystal Diffraction
Provides accurate 3D structures and functional information
Protein structure determination (screening, in-house data collection)
Proteins binding to drugs, DNA or other proteins
Small molecules in the bio-/pharma industry
  Structure determination
  Accurate bond lengths and angles
  Absolute stereochemistry
  Packing diagram and intermolecular contacts
  Phase Analysis (Temperature!)
Single crystals of pharmaceutical materials can often not be grown to a „sufficient" size!

## Slide 6: X-ray Diffraction
  Crystals are solid materials with atoms, molecules, or ions arranged in an orderly repeating pattern extending in all three dimensions.
  X-ray wavelengths are on the order of interatomic distances
    Molybdenum radiation: 0.71Å, Gallium radiation: 1.34Å Copper radiation: 1.54Å
    Carbon-carbon single bond: 1.54 Å.
  X-rays (electromagnetic waves) pass through the crystal as a diffraction grating and the resulting diffraction pattern is recorded on the CMOS detector.
X-ray Source
Crystal
Detector
Software
6
Structure

## Slide 7: Chemical & Biological Crystallography
D8 QUEST
D8 VENTURE

## Slide 8: Absolute configuration of molecules
(5R)-[(1S)-1,2-dihydroxy-ethyl]-3,4-dihydroxy-furan-2(5H)-one
L-Ascorbic acid
A
B
C
D
A
B
C
D
R
S
An absolute configuration in stereochemistry is the spatial arrangement of the atoms of a chiral molecular or group and its stereo-chemical description e.g. R or S.

## Slide 9: Typical examples

## Slide 10: Example of Biological Significance of Stereoisomers
enantiomers
(S)-(+)-carvone
(R)-(-)-carvone
smells like spearmint
smells like caraway

## Slide 11: Light atom structures
The reliable determination of the absolute structure of these compounds requires to detect small anomalous signals in the order of only 0.2 … 1%.

## Slide 12: (2S)-(−)-2,2′-Oxybis(octahydro-7,8,8-trimethyl-4,7-methanobenzofuran)
0.15 × 0.05 × 0.04 mm3
2175 frames were collected with a total exposure time of 4.14 hours
Data to 0.75 Å
96% complete, 4 fold redundant
R(int) = 3.68%
R1 = 3.18%, wR2 = 8.27%
<|F2anom|>/<F2> = 0.17%
Flack x = 0.024(39) (Parsons‘)
Absolute structure can be determined reliably
P21
a = 7.7975(2) Å, b = 12.8027(3) Å, c = 10.9201(3) Å
β = 101.9650(10)°

## Slide 13: Cytosine β-D-riboside, Cytidine
0.24 × 0.20 × 0.18 mm3
Total exposure time of 3 hours.
Data to 0.71 Å
97.4% complete, 7 fold redundant
R(int) = 10.88%
R1 = 2.73%, wR2 = 7.15%
<|F2anom|>/<F2> = 0.20%
Flack x = 0.00(3) (Parsons‘)
Absolute structure can be determined reliably
P212121
a = 5.0742(2) Å, b = 13.9292(6) Å, c = 4.7144(6) Å

## Slide 14: Cytosine β-D-riboside, Cytidine
Simulated precession pattern to 0.71Å
Invariom refinement R1 (INV) 1.77%

## Slide 15: Ligand binding studies
The structure of HIV protease, a viral enzyme critical in HIV’s life cycle, provided insight in how to block this enzyme. For most enzymes, made up of two equal halves, both halves have an active site, but HIV protease has only one active site, that, once blocked with a small molecule, could shut down the whole enzyme and theoretically stop the virus’ spread in the body by using the enzyme’s structural shape as a guide.
http://en.wikipedia.org/wiki/HIV-1_protease

## Slide 16: Ligand binding studies
The D8 VENTURE is an excellent system to quickly screen samples for bound ligands.
3-N-ACETYL TRANSFERASE
Source Bordetella petrii
Contains bound CoA
21 kD, 192 aa
Unit cell
a=68.5, b=108.0, c=91.1 Å
b=102.3
Space group: P21
Structure solved in Hazel Holden’s laboratory, University of Wisconsin

## Slide 17: Ligand binding studies
10 hour data set
Resolution 2.0 Å
Rmerge = 0.072 (0.25)
I/σI = 9.5 (2.8)
Multiplicity = 3.9 (2.0)
Fomfc map contoured at 3s (red density) clearly shows the position of the CoA ligand

## Slide 18: X-Ray Diffraction Techniques Powder Diffraction
Lead Finding
Optimization
Preclinical
Phase I
Phase II
Phase III
Marketing
XRPD
Discovery
Development
Production
SC-XRD

## Slide 19: From Discovery to Production Most Important XRPD Applications
Synthesis of new materials Phase ID, structure analysis
Solid-state characterisation
  Crystallinity Quant. analysis
  Thermal behaviour Phase ID
  Hygroscopic behaviour Phase ID
  Grindability / compressability Phase ID
  Polymorphism Phase ID, structure analysis
Quality control Phase ID, quant. analysis
Solid state reactions?
Lead Finding
Optimization
Preclinical
Phase I
Phase II
Phase III
Marketing
Discovery
Development
Production

## Slide 20: Why X-Ray Powder Diffraction?
Many materials first show up as powders
Many materials are available only as powders (polymorphism)
Non-ambient studies may be only possible with powders
...
Statistically relevant (representative of the bulk)!

## Slide 21: Why X-Ray Powder Diffraction
Polymorphism
Crystal habit/morphology
Crystal surfaces
Dissolution
Density
Flowability
Compressibility
Grindability
Hardness
Crystallinity
Activity
Stability
Hygroscopicity
…
Many material properties depend on crystal structure, e.g.:

## Slide 22: Why X-Ray Powder Diffraction
Phase Identification: It is the ability to unequivocally differentiate one crystallographic phase from another that proved to be the greatest asset in the pharmaceutical field
Quantitative Analysis: X-ray diffraction crystallographic techniques are increasingly used to detect, identify and quantify crystalline and amorphous phases
Structure Analysis: While thermal analysis and spectroscopy (IR, Raman, solid-state NMR) may be able to discriminate between an amorphous and a crystalline phase, these techniques cannot definitely characterize (the crystal structure of) polymorphic forms or solvates
Non-ambient Analysis: Can follow phase transitions and reactions in real time

## Slide 23: Why X-Ray Powder Diffraction?
Change of solvent may result in different polymorph
Scale up may lead
to a change in
crystal growth and
different polymorph
Drying or storing
may cause solid state reactions or phase transitions (T, RH, t)
Milling, tablet formation may result in phase transition (p)
Drug Product Performance

## Slide 24: Why X-Ray Powder Diffraction?
Nondestructive testing - without the need to dissolve, digest, or destroy the sample
Detection, identification and quantification of crystalline phases down to 0.05% possible
Detection, identification and quantification of amorphous phases down to less than 1% possible
Rietveld Structure determination and refinement
Analysis of final dosage forms
Accepted methodology for new product registrations and patent applications
...

## Slide 25: Phase Identification Polymorphism of Paracetamol
Nichols & Frampton (1998) J.Pharm.Sci. 87(6), 684-693

## Slide 26: Phase Identification - Tablet Screening Fortecortin®
Tablets measured in their original packing environment in transmission geometry

## Slide 27: Non-Ambient Phase ID (T, RH) Pocket Hydrate
Water is key to crystal lattice, on drying crystal lattice collapses
Chemically and physically unstable amorphous material produced
Storey, Pfizer Global R&D (2003) IWPCPS 4, www.assainternational.com, collected presentations

## Slide 28: Non-Ambient Phase ID (T, RH) Channel Hydrate
Water is present in channels and freely moves in and out of lattice
  Some changes to crystal lattice on dehydration but crystalline form remains at high-temperature
  Hydrate rapidly reforms on cooling
Storey, Pfizer Global R&D (2003) IWPCPS 4, www.assainternational.com, collected presentations

## Slide 29: Quantitative Phase Analysis API / Excipient
Lactose Hydrate
Paracetamol
Paracetamol : Lactose Hydrate // 85 : 15

## Slide 30: Quantitative Phase Analysis Telmisartane - Form Beta in Form Alpha
Form beta
Mixtures containing different concentrations of form beta are measured…
…a calibration curve is then plotted, and relative amounts of form beta in other mixtures can be determined.
Accuracy better than 0.2% for all samples

## Slide 31: Structure Determination
Solving molecular crystal structures from laboratory X-ray powder diffraction data with DASH: the state of the art and challenges
Florence et al. J. Appl. Cryst. (2005), 38, 249–259
D8 ADVANCE

## Slide 32: Instrumentation in XRPD D2 PHASER
Applications
Phase identification
Quantitative phase analysis (single peak methods)

## Slide 33: Instrumentation in XRPD D4 ENDEAVOR
Applications
Phase identification
Quantitative phase analysis (single peak methods)
Fully automated powder diffractometer with large sample handling system for high throughput analysis

## Slide 34: Instrumentation in XRPD D8 ADVANCE / D8 DISCOVER
Applications
Phase Identification
Quantitative Phase Analysis
Structure Determination and Refinement
PDF Analysis
Non-Ambient Analysis (p, T, rH)
Can be operated in transmission and reflection geometry

## Slide 35: Instrumentation in XRPD D8 DISCOVER
Applications
High-throughput of small sample amounts
  Combinatorial Screening
  Polymorph Screening
Tablet screening